Magmatic Ore Deposits

Mode of formation of orthomagmatic ores:

- fractional crystallization from melt

- liquid immiscibility between a sulfide liquid and the silicate melt.

- liquid immiscibility between an oxide liquid and the silicate melt

- liquid immiscibility between a carbonate liquid and the silicate melt

- Dissemination

- End stages of magmatic crystallization.

Elements concentrated by magmatic processes:

- PGM, Ni, Cu, Ti, V, Cr, diamonds, minor Fe

- REE, Nb, Zr, Li, Be, B, U, W, Sn, and Ta.

Types of orthomagmatic ores:

- Chromite

- Platinum Group Metals

- Cu-Fe-Ni sulfides

- Fe-Ti (± V) oxides

- Diamond in kimberlites

- REE, and Zr in carbonatites

- Pegmatites and Greisens:

Chromite Deposits

Types:

- Stratiform (Bushveld type; stable cratons)

- Podiform (Alpine type; orogenic; associated with ophiolites, or with Archean greenstone belts).

Uses of Chromite: (Cr/Fe ratio and Mg and Al contents are important; cf. Evans).

- Source of Cr, necessary for the steel industry

- Refractory

- Chemical industries

Characteristics of Startiform deposits:

  - Age: Precambrian

  - Tectonic setting: cratonic, rifted continental platforms

  - Great lateral extent (10’s of km), thickness: a few cm to a few meters.

  - Occur in funnel shaped igneous intrusions or huge sills or dykes. Rock associations include dunites, pyroxenites, and anorthosites.

  - Chromite is a cumulus phase in all rock types; but generally tends to concentrate with Opx (absence of cumulus Cpx is a favorable criterion).

  - Chromite seams occur at a stratigraphic level above which Opx first appears as a cumulus phase.

  - Believed to be a product of fractional crystallization from a highly magnesian melt (> 12% MgO)!

  - Cr/Fe, Mg/(Fe + Mg), and Cr/(Cr+Al+Fe3+) in the chromite decrease upsection.

  - Examples: Bushveld Complex; Great Dyke of Zimbabwe.

Origin:

- Crystal settling from a magma (inadequate!)

- Increase in fO2 due to explosive release of P, and loss of H2.

- Mixing of crystallizing magma with a fresh batch of less fractionated magma

- Mixing of crystallizing magma with a granitic melt (possibly a product of assimilation and partial melting of intruded roof rocks?)

Characteristics of Podiform deposits:

- Age: Paleozoic to Tertiary

- Lenticular bodies in ultramafic or mafic layers of ophiolite bodies; rarely exceeding 100 m in length.

- Associated with harzburgites and dunites; characteristic of fast spreading ridges, not slow ones!

- Best grade chromite; better than stratiform, but obviously of lower reserves.

Origin:

Partial melting of upper mantle rocks; magma withdrawn from pockets of melt; chromite crystallizes early and sinks back into these pockets; podiform shapes produced by flow of magmas, and other tectonic forces.